## Slide 1: Li-ion Battery thermal runaway ECN topic
ECN 9 workshop
Michele BARDI (IFPEN)
Antonio Garcia (CMT)
September 9th 2023, Napoli

## Slide 2: Li-ion Battery thermal runaway ECN Topic
ECN 9 workshop
Michele BARDI (IFPEN)
Antonio Garcia (CMT)
September 9th 2023, Napoli

## Slide 3: Thermal runaway topic
Li-ion battery thermal runaway is a challenging safety issue for mobility electrification
Why ECN is dealing with batteries?
  It concerns mobility
  It involves several phenomena that we know and we have the tools to study:
    Combustion
    Di- (or tri-) phasic jets
    Heat transfer
    Challenging condition testing (high temperature, short time scales)

## Slide 4: Thermal runaway topic
Li-ion battery thermal runaway is a challenging safety issue for mobility electrification
Why ECN is dealing with batteries?
  It concerns mobility
  It involves several phenomena that we know and we have the tools to study :
    Combustion : different and partially unknown fuels
    Di- (or tri-) phasic jets : fluid composition not constant, nozzle geometry “not cylindrical”
    Heat transfer: convection, radiation, conduction, flame propagation and runaway propagation
    Challenging condition testing (high temperature, short time scales): relevant boundary condition and parametric variation to be understood

## Slide 5: Thermal runaway topic
Combustion community is starting to study Li-ion thermal runaway
  Experimentally and numerically
The topic objectives:
  Apply the “Spray A” approach to the test currently performed
    optical characterization of thermal abuse
    Start investigating results “dispersion” / lab to lab bias
  To form a “peloton” on the subject
    Share good experimental / modeling practice
    It seems to be a wide world to explore (much more parameters to investigate / much more boundary conditions to explore)
    Generate a virtuous exchange between combustion and battery communities

## Slide 6: Thermal runaway topic
A reference case has been defined
  Reference battery + reference abuse test
  5 lab volunteered to perform tests (CMT, IFPEN, KAUST, University of Tennessee, KIT)
    Only two labs managed to perform experiment due to shipping / schedule issue
  Comparison of results to reference test approach
  Hints on possible optical analysis
A community is forming around the topic
  2 pre-workshop meetings / technical exchanges
  Possibility to start the discussion on future direction
  Discussion of practical issue (e.g. battery shipment issues..)
  Identification of possible way of participating to the topic

## Slide 7: Thanks to all Contributors!

## Slide 8: Agenda
Experimental activities Reference case description and discussion of the available data
    Abuse test description
    Abuse test comparison
    Complementary analysis on reference cells
  ARC for battery thermal runaway investigation (KIT)
  Lessons from recent studies on battery thermal runaway (University of Tennessee)
Numerical results:
  3-D approach (Converge)
  0-D/1D numerical Approach(CMT / IFPEN)
In parallel please fill in the Beekast Survey:
  Which are the key measurement that we should / could add to reference battery cell case?
  On which aspect of our results, we should be focusing on the most?
  How should reference case evolve?
    Battery cell Geometry
    Abuse test
    Ageing process
    …
  How to investigate to cell-to-cell propagation?

## Slide 9: Reference case
Common battery chosen
  LG M50LT from the same production lot
  120 battery cells purchased and shared by IFPEN
Reference Running-in
  3 charge / discharge cycles
  CC/CV ref cycle from manufacturer
Test Definition:
  Thermal Abuse
  “Slow cooking mode”
    Heating with a controlled heating ramp at constant gradient
    Reference case : 1.5 °C/min
    Parametric Variation: 0.5 °C/min ; 0.2 °C/min
  BC state of charge (SOC):
    Ref Case: 100%
    Parametric variations: 50% ; 25% ; 75%

## Slide 10: Experimental campaign
Experimental campaign on ARC at IFPEN HWS using the reference battery used for comparison (SAE 2023-24-160)
IFPEN / CMT |  | SOC |  |  | 
 |  | 25% | 50% | 75% | 100%
Heating Ramp | 0,5°C/min | 0 / 0 | 3 / 3 | 0 / 0 | 3 / 3
 | 1,5°C/min | 3 / 0 | 3 / 3 | 3 / 0 | 7 / 4
ARC | HWS : 5°C – 30min - 0.02 °C/min |  | 3 | 2 | 5

## Slide 11: Setup Description: CMT setup
Adapted ARC
Double heating system:
  Electrical resistance in contact with the cell
  ARC resistance in « Exothermic mode » to keep ambient air at skin temperature
Temperature measurement at
  Skin temperature
  Gas temperature 1 cm over the cap
Laser triggered camera
Trigger system with laser

## Slide 12: Setup description : IFPEN setup
Adapted CV vessel
Electrical heating of the vessel body
  Air temperature homogenized by a fan
  Cell heating by convection
Constant air flux for gas analysis
  0.25 l/min to have low impact on temperature
Capillary system at the outlet to detect cell gas emissions
High speed cameras
  Simultaneous Schlieren + natural luminosity

## Slide 13: Sample Test results
Global runaway description measurement :
Richardet et al, SAE 2023-04-0165
García, et al., Energy Conversion and Management 2021
The following main events are in general described during TR in a thermal abuse case
1. Exothermic reaction onset
  -Observed mainly with HWS method
2. Voltage drop : CID (current interrupting device) stop battery form charge/decharge (non reversible)
3. Gas Venting
- Temperature variation
- Pressure increase
-Gas Analysis
Voltage Drop
Gas Venting
Exothermic
onset

## Slide 14: Sample Test results
Global runaway description measurement :
Richardet et al, SAE 2023-04-0165
García, et al., Energy Conversion and Management 2021
The following main events are in general described during TR in a thermal abuse case
1. Exothermic reaction onset
  -Observed mainly with HWS method
2. Voltage drop : CID (current interrupting device) stop battery form charge/decharge (non reversible)
3. Gas Venting
- Temperature variation
- Pressure increase
-Gas Analysis
-Video Analysis
M50 / SOC 50% / 1.5°C/min
Di-(Tri) phasic jet
Complex nozzle
~100 ms duration
Gas Venting
S. Ohneseit, P. Finster, C. Floras, N. Lubenau, N. Uhlmann, H.J. Seifert, C. Ziebert, Batteries 2023, 9, 237, https://doi.org/10.3390/batteries9050237
M50 2018
M50 2019

## Slide 15: Sample Test results
Global runaway description measurement :
Richardet et al, SAE 2023-04-0165
García, et al., Energy Conversion and Management 2021
The following main events are in general described during TR in a thermal abuse case
1. Exothermic reaction onset
  -Observed mainly with HWS method
2. Voltage drop : CID (current interrupting device) stop battery form charge/decharge (non reversible)
3. Gas Venting
4. Thermal Runaway
TR onset
Gas Venting
Exothermic
onset

## Slide 16: Sample Test results
Global runaway description measurement :
Richardet et al, SAE 2023-04-0165
García, et al., Energy Conversion and Management 2021
The following main events are in general described during TR in a thermal abuse case
1. Exothermic reaction onset
  -Observed mainly with HWS method
2. Voltage drop : CID (current interrupting device) stop battery form charge/decharge (non reversible)
3. Gas Venting
4. Thermal Runaway
Gas emission
Ignition
Incandescent particles
Optical thick gas/dust
M50 / SOC 100% / 1.5°C/min
~1 second duration

## Slide 17: Sample Test results
Global runaway description measurement :
Richardet et al, SAE 2023-04-0165
García, et al., Energy Conversion and Management 2021
The following main events are in general described during TR in a thermal abuse case
1. Exothermic reaction onset
  -Observed mainly with HWS method
2. Voltage drop : CID (current interrupting device) stop battery form charge/decharge (non reversible)
3. Gas Venting
4. Thermal Runaway
Gas emission
Ignition
Incandescent particles
Optical thick gas/dust

## Slide 18: Reference case
IFPEN
CMT
7 tests repetitions
4 tests repetitions
venting
Skin temperature
T gradient vs Temperature
At venting an important temperature reduction is observed by CMT
  TC position : IFPEN at mid height / CMT at upper part (no contact with jet)
TR gradient behavior is clearly different
  The transition to thermal runaway significantly different in the two cases
    In CMT experiments the battery cell-air heat exchange is limited (holder + heating mode)
    The TR temperatures at IFPEN are lower air might have a cooling effect on battery skin

## Slide 19: Heating ramp and heating control
Heating ramp: 1.5 °C/min
IFPEN
CMT
Heating ramp: 0.5 °C/min
Heating ramps are reasonably close to the target ramps
However, for both cases a deviation from the target is observed starting at 120°C
  Evident for CMT, but detectable also in IFPEN data
  Potential interesting measurement for future
ARC results detects exothermic reaction onset at T >70°C

## Slide 20: SOC 100 comparison: skin temperature measurement
Heating ramp: 1.5 °C/min
IFPEN
CMT
Heating ramp: 0.5 °C/min
The reduction in heating ramp slope has an obvious effect on venting and TR time
Delay between Venting and TR increases more for IFPEN
  In both case is less than 3 times longer (3 times lower heating ramp)
  Combination of heating ramp and chemical reactions time
7 tests repetitions
4 tests repetitions

## Slide 21: Venting and runaway temperatures
Consistent deviation Voltage drop temperature between ref ARC and IFP – HPHT
  Related to the CID design
Venting and runaway temperatures are often evaluated to describe Thermal runaway behavior
  Variability observed is acceptable and enable to identify clear trends (effect of SOC)
  Agreement with reference method (ARC HWS mode)
  At lower heating rate
    Results variability increases significantly
    Impact of heating strategy become bigger at slow heating rate
    Minor impact on the characteristic temperatures

## Slide 22: Max skin temperature
Max skin temperature measurement can provide information on the intensity of the TR event
  Dispersion obtained is very large
  Need to find more responsive sensors
  Could this be an effective variability of temperature?

## Slide 23: Venting video observation
Venting jet penetration is very fast
  High sampling rate: in 300µs is out of field of view
  Larger field of view is needed
  Liquid and vapor could provide different answers
1.5 °C/ min heating ramp / 100 SOC
IFPEN NL / Mie scattering

## Slide 24: Venting video observation
Effect of SOC on venting seems to be affected by SOC
  statistical analysis is needed
  The way in which safety valve brakes can affect jet development
SOC50%
0 us
200 us
400 us
600 us
800 us
1000 us
1200 us
1400 us
1600 us
1800 us
SOC100%

## Slide 25: SOC effect on videos
At 100% SOC ignition takes place immediately after the gas ejection (~0.3 ms)
At 50% SOC it take longer (~ 10 ms)
The ignition position might change significantly
In IFPEN movies no ignition is detected at 25% SOC
SOC 100%
SOC 50%
CMT 1.5 °C/ min heating ramp

## Slide 26: Reference case experiment Conclusions 1/2
Temperature ramp abuse test was carried out in two different optically accessible facility
  Heating strategy was not the same and it has an important effect on the transient before TR
Characteristic temperatures can be characterized via different techniques, are compared to ARC reference HWS results
  Exothermic onset temperature is still missed “T ramp” case
  VD temperature is consistently higher in “T ramp” case
  Venting and TR onset temperature are comparable (in absolute values and trend)
  Results variability is acceptable:
    SOC trend could be identified
    T ramp slope affect the variability of the results
    Important to perform test repetitions
Important information about heat release can be studied via pressure analysis (not presented / not ready)

## Slide 27: Reference case experiment Conclusions 2/2
High speed videos provide important information to understand the process
  Venting
    Complex jet shape strongly depending on battery type: which are the key measurement to perform?
    “venting valve” to be characterized for the current battery
    Orientation of battery should be clarified
    Larger field of view would be beneficial to characterize the process
  TR
    A continuous gas emission could be observed from venting until TR
    Via NL jet ignition is shown to take place in different ways (directly at the vent cap in a ”diffusive” outlet or far from it followed by a “flame propagation”)
    OH* images, combined with high-speed pressure measurement could clarify the ignition process
    SOC affect significantly TR and the ignition detection
    Optical thick Smoke make it difficult the visualization of the event

## Slide 28: Agenda
Experimental activities Reference case description and discussion of the available data
    Abuse test description
    Abuse test comparison
    Complementary information and analysis on reference cells
  ARC for battery thermal runaway investigation (KIT)
  Lessons from recent studies on battery thermal runaway (University of Tennessee)
Numerical results:
  3-D approach (Converge)
  0-D/1D numerical Approach(CMT / IFPEN)
In parallel please fill in the Beekast Survey:
  Which are the key measurement that we should / could add to reference battery cell case?
  On which aspect of our results, we should be focusing on the most?
  How should reference case evolve?
    Battery cell Geometry
    Abuse test
    Ageing process
    …
  How to investigate to cell-to-cell propagation?

## Slide 29: Battery cells tested
LG INR21700LT M50 => « M50 »
70 cm
2,1 cm
/ 3.69V
2,1 cm
  Cnom = 4,85 Ah
  Energy density = 263 Wh/kg
Notes: 21700 format cylindrical
Capacity of almost 5Ah
Energy density of 263 Wh/kg

## Slide 30: Battery cells tested
X. Feng, M. Ouyang, X. Liu, L. Lu, Y. Xia, X. He, Thermal runaway mechanism of lithium ion battery for electric vehicles: A review, Energy Storage Materials 10 (2018) 246–267.
  State of the art cylindrical battery cell
LG INR21700LT M50 => « M50 »
70 cm
2,1 cm
2,1 cm
263 Wh/kg
Notes: That kind of energy density => state of the art battery
Lead to specific electrode chemistry

## Slide 31: Composition
Positive Electrode
  NMC 811 (not specific to M50)
Negative Electrode
  Graphite/Silicon
  Weight percentage of graphite and silicon oxide is 90% and 10% by weight (Chen, 2020)
  Si 1% in weight of the battery cell mass (Popp, 2021)
Electrodes
Top-view EDS images of the negative electrode extracted from LGM50 displaying graphite (red) and silicon oxide (green) content.
Chen, 2020
Chen, 2020
Notes: NMC 811 => 80% Nickel 10% Manganese 10% Cobalt
Ni-rich
Silicon at the anode to boost the capacity of the battery
NE Active material is around 7g ~10% of total mass of BC

## Slide 32: Composition
LiPF6 (Catenaro, 2021)
Organic solvent (Ohneseit, 2023, KIT)
  Important to perform the same kind of analysis for our generation of M50 (2022)
Electrolyte + Solvant
M50 : generation 2018
Notes: Lithium salts LiPF6 similar to most of LIB
Organic Solvant
DMC, EMC and EC according to KIT work
Keep in mind it is a 2018 generation and we have a 2022 one

## Slide 33: Advanced gas analysis at IFPEN
Experimental setup – ongoing activity
Capillary
Air/N2
Alicat
Q =0.25 L.min-1
7-bar air network
Alicat
Q =17 L.min-1
scavenging
T°
P
Filter
Exhaust Line
7-bar air network
Combustion Gas
Pneumatic valve
Lambda
VHPHT = 1,4 L
P
7 L.min-1
7-Gas Analyzer (Horiba)
5 L.min-1
Particle Analyser (Pegasor)
Some gas emitted can be really hazardous
  HF can be formed
  Quantify these emissions
  Trap them to avoid damaging analyzers
  Yang, 2006
  Kawamura, 2006
  Use of Bubblers
Mass flow
Venting
Runaway
PUMP
Bubblers
Mass flow
PUMP
Exhaust
Notes: Toxic gases can be found, harmful for health or also for some analyzers
Especially Hydrogen Fluoride
Need to quantify the risks and try to trap them => bublers to dissolve the HF into it

## Slide 34: Experimental Set up
Detect hazardous gases
Results
100% SOC M50 battery cells were tested (Ionic Chromatography)
  No trace of HF have been detected
  Bubblers were removed
Capillary
Air/N2
Alicat
Q =0.25 L.min-1
7-bar air network
Alicat
Q =17 L.min-1
scavenging
T°
P
Filter
Exhaust Line
7-bar air network
Combustion Gas
Pneumatic valve
Lambda
VHPHT = 1,4 L
P
7 L.min-1
7-Gas Analyzer (Horiba)
5 L.min-1
Particle Analyser (Pegasor)
Mass flow
Venting
Runaway
PUMP
Bubblers
Mass flow
PUMP
Exhaust
Notes: 100% SOC M50 tested and no trace of HF found in Ionic Chromatography =>so we removed the bublers

## Slide 35: Experimental Set up
Collect gases
Capillary
Air/N2
Alicat
Q =0.25 L.min-1
7-bar air network
Alicat
Q =17 L.min-1
scavenging
T°
P
Filter
Exhaust Line
7-bar air network
Combustion Gas
Pneumatic valve
Lambda
VHPHT = 1,4 L
P
7 L.min-1
7-Gas Analyzer (Horiba)
5 L.min-1
Particle Analyser (Pegasor)
Mass flow
Venting
Runaway
PUMP
Mass flow
PUMP
Exhaust
Venting Bag
TR Bag
Gas collection
  100% SOC M50
  during 1 min after Venting and Thermal Runaway
  Collected from exhaust line at 2 L.min-1
  Dilution of the vent gases via mass flowmeter 17 L.min-1
  Dilution of the vent gases via mass flowmeter 2 L.min-1
Q =2 L.min-1
Notes: We Tested LIB in same condition 100% SOC
Collection 1 min after Venting for 1 bag and 1 min after TR in a second bag
We regulated on the second and third test our dilution of exhaust gases

## Slide 36: GAS collected analysis
Echantillon : | 23-03498-2 | 23-03498-4 | 23-03498-6
Peak Name |  | Relative Area (%) | 
Ethane | 3.57 | 1.56 | 1.29
Water | 6.05 | 0.69 | 0.76
Propyne | 0.06 | 0.04 | 0.03
Silane, difluorodimethyl- | 0.04 | 0.05 | 0.03
Acetaldehyde | 0.11 | 0.04 | 0.09
Methyl Alcohol | 0.1 | 0.06 | 0.15
1-Propene, 2-methyl- | 0.31 | 0.19 | 0.22
1,3-Butadiene | 1.72 | 1.34 | 0.92
2-Butene | 0.13 | 0.07 | 0.09
Trimethylsilyl fluoride | 1.17 | 0.75 | 0.76
2-Butene, (Z)- | 0.1 | 0.07 | 0.07
1-Pentene | 0.05 | 0.02 | 0.02
Acetic acid, methyl ester | 0.05 | 0.1 | 0.06
1,3-Cyclopentadiene | 0.26 | 0.15 | 0.2
Silanol, trimethyl- | 0.37 | 0.03 | 0.4
1-Hexene | 0.06 | 0.02 | 0.02
Carbonic acid, dimethyl ester | 63.19 | 82.56 | 71.09
Tetrahydrofuran | 0.19 | 0.19 | 0.17
Dimethyl-(allyl)-silyloxybenzene | 0.07 | 0.03 | 0.08
Benzene | 15.93 | 5.02 | 15.12
Carbonic acid, ethyl-, methyl ester | 4.05 | 4.75 | 4.44
Disiloxane, hexamethyl- | 0.66 | 0.3 | 0.96
Toluene | 0.31 | 0.06 | 0.26
Cyclotrisiloxane, hexamethyl- | 1.07 | 0.24 | 1.12
Trisiloxane, octamethyl- | 0.06 | 0.02 | 0.08
Cyclotetrasiloxane, octamethyl- | 0.08 | 0.02 | 0.04
GC-MS
Qualitative detection of many species
  3 tests were conducted on 100% SOC
Echantillon : | 23-03498-1 | 23-03498-4 | 23-03498-3 | 23-03498-6 | 23-03498-5
Peak Name | Relative Area (%) | Relative Area (%) |  |  | 
Water | 87.74 | 80.65 |  | 79.99 | 
Carbonic acid, dimethyl ester | 11.91 | 19.35 |  | 17.17 | 
Benzene | 0 | 0 |  | 0.76 | 
Carbonic acid, ethyl-, methyl ester | 0.35 | 0 |  | 2.08 | 
Venting Bag
Thermal Runaway Bag
DMC
EMC
Silicon based gases
Notes: Give data that are quite repetable over the 3 tests
Mostly water during Venting
3 intersting point in TR
DMC, EMC and silicon based gases

## Slide 37: GAS collected analysis
Echantillon : | 23-03498-2 | 23-03498-4 | 23-03498-6
Peak Name |  | Relative Area (%) | 
Ethane | 3.57 | 1.56 | 1.29
Water | 6.05 | 0.69 | 0.76
Propyne | 0.06 | 0.04 | 0.03
Silane, difluorodimethyl- | 0.04 | 0.05 | 0.03
Acetaldehyde | 0.11 | 0.04 | 0.09
Methyl Alcohol | 0.1 | 0.06 | 0.15
1-Propene, 2-methyl- | 0.31 | 0.19 | 0.22
1,3-Butadiene | 1.72 | 1.34 | 0.92
2-Butene | 0.13 | 0.07 | 0.09
Trimethylsilyl fluoride | 1.17 | 0.75 | 0.76
2-Butene, (Z)- | 0.1 | 0.07 | 0.07
1-Pentene | 0.05 | 0.02 | 0.02
Acetic acid, methyl ester | 0.05 | 0.1 | 0.06
1,3-Cyclopentadiene | 0.26 | 0.15 | 0.2
Silanol, trimethyl- | 0.37 | 0.03 | 0.4
1-Hexene | 0.06 | 0.02 | 0.02
Carbonic acid, dimethyl ester | 63.19 | 82.56 | 71.09
Tetrahydrofuran | 0.19 | 0.19 | 0.17
Dimethyl-(allyl)-silyloxybenzene | 0.07 | 0.03 | 0.08
Benzene | 15.93 | 5.02 | 15.12
Carbonic acid, ethyl-, methyl ester | 4.05 | 4.75 | 4.44
Disiloxane, hexamethyl- | 0.66 | 0.3 | 0.96
Toluene | 0.31 | 0.06 | 0.26
Cyclotrisiloxane, hexamethyl- | 1.07 | 0.24 | 1.12
Trisiloxane, octamethyl- | 0.06 | 0.02 | 0.08
Cyclotetrasiloxane, octamethyl- | 0.08 | 0.02 | 0.04
GC-MS
DMC and EMC are components of the electrolyte
  Also found in Abbott et al. work (2022)
  No trace of EC which was detect on ante mortem analysis (Ohneseit, 2023, KIT)
Silicon based gases probably coming from Negative electrode decomposition
Thermal Runaway Bag
DMC
EMC
Silicon based gases
  This is a step forward, but need to quantify the emissions
Notes: DMC and EMC are found also in Abbott M50 gas analysis in thermal abuse
Similar to KIT ante mortem analysis , laking EC
Silicon from Negative electrode
Now we lack quantification

## Slide 38: Perspectives
Capillary
Air/N2
Alicat
Q =0.25 L.min-1
7-bar air network
Alicat
Q =17 L.min-1
scavenging
T°
P
Filter
Exhaust Line
7-bar air network
Combustion Gas
Pneumatic valve
Lambda
VHPHT = 1,4 L
P
7 L.min-1
7-Gas Analyzer (Horiba)
5 L.min-1
Particle Analyser (Pegasor)
FTIR
Measurement
3.8 L/min
Some data in the literature
BUT really chemistry dependent AND probably generation dependent
So we are aiming for a set up to characterize the emission over time with FTIR analyzer
  Need for others to join the efforts